ADDRESS: 581 A, A, Riico Industrial Area, Bhiwadi, TEH, Tijara, Alwar, Rajasthan, 301019

(Manufacturers of All Types PVC Compounds)

PERIWAL POLYTECH PVT. LTD.

Website: periwalpolytech.com

=

| Periwal Polytech Private limited ( PVC Compounds) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Automotive Molding and Profile Grades |  |  |  |  |  |  |  |  |  |  |
| Properties | Color | Specific Gravity | Hardness ( Shore A) | Thermal stability@ 200 0C | Tensile strength | Elongation at Break | Volume Resistivity | Izod Impact | Application |
| Unit |  |  | Nos. | Minutes (Min.) | Mpa (Min.) | % (Min.) | Ohm-Cm | Kgf.cm/cm |  |
| Test method | Visual | ASTM D792 | ASTMD 2240 | IS 5831 | ASTM D 638 IS 10810 (Part 7) |  | ASTM D 4325 | ASTM D 256 |  |
| Grade |  |  |  |  |  |  |  |  |  |
| PPL 245 ATN | Natural | 1.28±0.03 | 44±3 | 80 | 4 | 300 | NA | NA | Two-wheeler Handle Grip |
| PPL 201AT | White | 1.50±0.03 | 80±3 | 80 | 10 | 250 | NA | NA | Automotive Profile |
| PPL 265 NBR | Black | 1.35±0.03 | 65±3 | 80 | 8 | 400 | NA | NA | Rubberized Automotive Molding |
| PPL 245 W | White | 1.28±0.03 | 44±3 | 50 | 3 | 300 | NA | NA | Two-wheeler Handle Grip |
| PPL 245 WPF | White | 1.30±0.03 | 53±3 | 50 | 5 | 250 | NA | NA | Phthalate free Two-wheeler Handle Grip |
| PPL 255 K PF | Black | 1.37±0.03 | 58±3 | 80 | 7 | 300 | NA | NA | Automotive Molding (Phthalate free) |
| PPL 265 K PF | Black | 1.48±0.03 | 66±3 | 80 | 8 | 300 | NA | NA | Automotive Molding (Phthalate free) |
| PPL 255 KPFS REACH | Black | 1.43±0.03 | 60±3 | 80 | 6 | 300 | NA | NA | Automotive Molding (REACH) |
| PPL 260 KEC | Black | 1.60±0.03 | 60±3 | 50 | 5 | 250 | NA | NA | Automotive Molding |
| PPL 280 KLF | Black | 1.27±0.03 | 70±3 | 60 | 12.5 | 300 | NA | NA | Automotive Profile |
| PPL 2233 K | Black | 1.50±0.03 | 58±3 | 80 | 4 | 300 | NA | NA | Automotive Molding |
| PPL 275 SR | Black | 1.30±0.03 | 75±3 | 30 | 16 | 300 | NA | NA | Skipping cord |
| PPL 275 SR RED | Red | 1.32±0.03 | 75±3 | 30 | 16 | 300 | NA | NA | Skipping cord |
| PPL 275 SRG | Silver Grey | 1.32±0.03 | 75±3 | 30 | 16 | 300 | NA | NA | Skipping cord |
| PPL 275 SR RED T | Transparent Red | 1.30±0.03 | 75±3 | 30 | 16 | 300 | NA | NA | Skipping cord |
| PPL 203 ATN | Natural | 1.57±0.03 | 82±3 | 50 | 10 | 200 | NA | NA | Automotive Sleeve |
| PPL 203 KAT | Black | 1.57±0.03 | 82±3 | 50 | 10 | 200 | NA | NA | Automotive Sleeve |
| PPL 245 KEC | Black | 1.48±0.03 | 48±3 | 30 | 3 | 250 | NA | NA | Automotive Molding |
| PPL 270 ROHS | Black | 1.55±0.03 | 70±3 | 40 | 8 | 250 | NA | NA | Automotive Sleeves, Clutch wire, Chain Swing Arm |
| PPL 203 SE | Black | 1.40±0.03 | 69±3 | 50 | 8 | 300 | NA | NA | Automotive Molding (Gear Shift Knob etc.) |
| PPL 201 SE | Black | 1.40±0.03 | 42±3 | 50 | 2 | 250 | NA | NA | Two-Wheeler Molded Parts (Air Hose, Handle, Lever, etc.) |
| PPL 205 K | Black | 1.40±0.03 | 52±3 | 50 | 5 | 350 | NA | NA | Soft Automotive Molding (Gear Boot, Handle Grip, Bellows) |