PERIWAL POLYTECH PVT. LTD.

(Manufacturers of All Types PVC Compounds)

ADDRESS: 581 A, A, Riico Industrial Area, Bhiwadi, TEH, Tijara, Alwar, Rajasthan, 301019

Website: periwalpolytech.com

=

| Medical and Food ( Non Toxic) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Properties | Color | Specific Gravity | Hardness (Shore A) | Thermal stability@ 200 0C | Tensile strength | Elongation at Break | Volume Resistivity | Izod Impact | Application |
| Unit |  |  | Nos. | Minutes (Min.) | Mpa (Min.) | % (Min.) | Ohm-Cm | Kgf.cm/cm |  |
| Test method | Visual | ASTM D792 | ASTMD 2240 | IS 5831 | ASTM D 638 IS 10810 (Part 7) |  | ASTM D 4325 | ASTM D 256 |  |
| Grade |  |  |  |  |  |  |  |  |  |
| PPL 350 SMTKH | Black | 1.30±0.03 | 55±3 | 25 | 5 | 300 | NA | NA | Soft Gasket |
| PPL 355 TBL | Transparent Blue Tinge | 1.17±0.03 | 55±3 | 20 | 8 | 300 | NA | NA | Handle grip |
| PPL 360 T | Transparent | 1.26±0.03 | 60±3 | 20 | 10 | 350 | NA | NA | Handle grip |
| PPL 307T-EC | Transparent Blue Tinge | 1.28±0.03 | 70±3 | 20 | 14 | 300 | NA | NA | Drain tube |
| PPL 307 T | Transparent | 1.23±0.03 | 76±3 | 20 | 15 | 250 | NA | NA | Medical tubing |
| PPL 375 CL-6 | Transparent Blue Tinge | 1.20±0.03 | 75±3 | 20 | 15 | 350 | NA | NA | Medical tubing as Per USP Class-VI |
| PPL 380 TBL-EC | Transparent Blue Tinge | 1.28±0.03 | 75±3 | 20 | 15 | 250 | NA | NA | LED lights |
| PPL 380 T | Transparent Blue Tinge | 1.23±0.03 | 80±3 | 20 | 15 | 250 | NA | NA | Medical tubing |
| PPL 380 TN | Transparent | 1.23±0.03 | 80±3 | 20 | 15 | 250 | NA | NA | Medical Soft tubing |
| PPL 327 T | Transparent | 1.19±0.03 | 63±3 | 25 | 10 | 350 | NA | NA | Medical Soft tubing |
| PPL 325 T | Transparent | 1.20±0.03 | 67±3 | 30 | 12.5 | 250 | NA | NA | Medical Soft tubing |
| PPL 325 T PF | Transparent | 1.20±0.03 | 67±3 | 30 | 12.5 | 250 | NA | NA | Phthalate free soft medical tubing |
| PPL 374 LSMN | Transparent Blue Tinge | 1.23±0.03 | 74±3 | 20 | 12 | 300 | NA | NA | Oxygen mask |
| PPL 385 T | Transparent Blue Tinge | 1.23±0.03 | 85±3 | 20 | 15 | 250 | NA | NA | Medical tubing |
| PPL 380 TL6 | Translucent | 1.22±0.03 | 80±3 | 50 | 15 | 300 | NA | NA | Drain tube |
| PPL 4313 TN | Transparent Green | 1.32±0.03 | 70±3 (Shore D) | 30 | 30 | 30 | NA | NA | Tool grip |
| PPL 4313 TGR | Transparent Green | 1.32±0.03 | 70±3 (Shore D) | 30 | 30 | 30 | NA | NA | Tool grip |
| PPL 4313 TY | Transparent Yellow | 1.32±0.03 | 70±3 (Shore D) | 30 | 30 | 30 | NA | NA | Tool grip |